## Slide 1
Wire + Arc Additive Manufacturing of unalloyed tantalum
Marinelli G., Martina F., Ganguly S., Williams S.
28th International Solid Freeform Fabrication Symposium

## Slide 2: Agenda
Additive Manufacturing Processes Comparison
Capability of Wire + Arc Additive Manufacturing (WAAM)
Refractory Metals Deposition
- Development of WAAM for unalloyed tungsten
- Development of WAAM for unalloyed tantalum
- Functionally graded structure molybdenum to tungsten
Conclusion

## Slide 3: Additive Manufacturing Processes Comparison
Beam
Laser
Wire
Powder
Powder bed
Selective Laser Melting
Blown powder
Laser Cladding
Electron beam
Powder bed
Electron Beam Melting
Arc
TIG, MIG, Plasma
Wire
Wire+Arc AM
Wire
Sciaky
Powder
Cranfield University
Heat sources
Feedstock

## Slide 4: Additive Manufacturing Processes Comparison
Note – our assessment

## Slide 5: Capability of WAAM – Process
Thin wall revolving structures: ARA beanie
Building time: 2.5 hours
Wall thickness: around 5mm
Material: Al5087

## Slide 6: Capability of WAAM - Features
Inclined torch (CMT)
Angled and horizontal walls
Straight near net shape Ti thin wall
Machined intersections
Medium complexity 2D part
Weight efficient structure
With mixed materials

## Slide 7: Capability of WAAM – Semi-finished parts
1 metre
0.7 metre
24 kg

## Slide 8: Capability of WAAM - Materials
Ti-6Al-4V
  Grade 5
  Grade 23
Aluminium
  2024
  2319
  4043
  5087
Refractories
  Tungsten
  Molybdenum
  Tantalum
Invar
Steels
  ER60
  ER80
  ER90
  ER120
  Maraging grade 250
  Maraging grade 350
  Stainless (17-4 PH, 316L)
  Invar
Inconel
  625
  718
Bronze
Copper

## Slide 9
Refractory Metals Deposition

## Slide 10: Our final aims
W
Mo
W/Mo FGS

## Slide 11: Challenges of depositing refractory metals
High melting point;
High density;
Ductile-to-brittle temperature transition above room temperature.
High susceptibility to oxidation.
A completely inert atmosphere is required during deposition. A lot of heat is required to melt the feedstock and the substrate.

A lot of thermal stress applied to the deposit.

Ease of cracking.

## Slide 12: Challenges of depositing refractory metals (brittleness of tungsten)
Tungsten Deposited
via WAAM
Tungsten Substrate
produced via Powder
Metallurgy route

## Slide 13: Challenges of depositing refractory metals (managing heat accumulation)

## Slide 14: Development of WAAM for unalloyed tungsten

## Slide 15: Development of WAAM for unalloyed tungsten
Sound deposition achieved with ~ 6.1 kJ/mm
Deposition rate: 2.7 kg/h
Tungsten WAAM Deposition Parameters | 
Wire feed speed (WFS) | 35 mm s-1
Travel speed (TS) | 2 mm s-1
Current (I) | 350 A
Wire diameter | 1 mm
120 mm
80 mm
First structure ever in unalloyed tungsten using WAAM
Absence of cracks
Absence of oxidation

## Slide 16: Development of WAAM for unalloyed tantalum
Tantalum WAAM Deposition Parameters | 
Wire feed Speed (WFS) | 60 mm s-1
Travel Speed (TS) | 4 mm s-1
Current (I) | 300 A
Wire diameter | 1.2 mm
Sound deposition achieved with
~2.6 kJ/mm
Deposition rate:
4 kg/h
First structure ever in unalloyed tantalum produced via WAAM
230 mm
150 mm

## Slide 17: Development of WAAM for unalloyed tantalum
Chart: YS
| P Vertical | P Horizontal | H Vertical | H Horizontal | Substrate
 | 204 | 232 | 197 | 208 | 182
Chart: UTS
| P Vertical | P Horizontal | H Vertical | H Horizontal | Substrate
 | 231 | 261 | 218 | 227 | 240
Chart: Elongation
| P Vertical | P Horizontal | H Vertical | H Horizontal | Substrate
 | 27 | 38 | 38 | 32 | 62

## Slide 18: Development of WAAM for unalloyed tantalum (high pressure rolling)

## Slide 19: Development of WAAM for unalloyed tantalum

## Slide 20: Functionally graded structure molybdenum to tungsten
Chart: Composition [wt%]
| 34.979999999999997 | 34.42 | 43.13 | 55.78 | 56.89 | 73.56 | 75.069999999999993 | 82.179999999999978 | 83.02 | 87.76 | 88.56 | 89.09 | 91.5 | 91.98 | 93.78 | 92.84 | 92.51 | 80.86 | 77.459999999999994 | 63.17 | 54.35 | 50.21 | 47.68 | 37.08 | 32.86 | 22.24 | 18.05 | 14.92 | 12.99 | 9.120000000000001 | 9.8000000000000007 | 9.75 | 5.51 | 5.85 | 5.46 | 3 | 3.35 | 3.27 | 3.39 | 3.63 | 3.8 | 3.72 | 3.3
Mo | -1750 | -1500 | -1250 | -1000 | -750 | -500 | -250 | 0 | 250 | 500 | 750 | 1000 | 1250 | 1500 | 1750 | 2000 | 2250 | 2500 | 2750 | 3000 | 3250 | 3500 | 3750 | 4000 | 4250 | 4500 | 4750 | 5000 | 5250 | 5500 | 5750 | 6000 | 6250 | 6500 | 6750 | 7000 | 7250 | 7500 | 7750 | 8000 | 8250 | 8500 | 8750 | 9000 | 9250 | 9500 | 9750 | 10000 | 10250 | 10500
Ta | -1750 | -1500 | -1250 | -1000 | -750 | -500 | -250 | 0 | 250 | 500 | 750 | 1000 | 1250 | 1500 | 1750 | 2000 | 2250 | 2500 | 2750 | 3000 | 3250 | 3500 | 3750 | 4000 | 4250 | 4500 | 4750 | 5000 | 5250 | 5500 | 5750 | 6000 | 6250 | 6500 | 6750 | 7000 | 7250 | 7500 | 7750 | 8000 | 8250 | 8500 | 8750 | 9000 | 9250 | 9500 | 9750 | 10000 | 10250 | 10500
W | -1750 | -1500 | -1250 | -1000 | -750 | -500 | -250 | 0 | 250 | 500 | 750 | 1000 | 1250 | 1500 | 1750 | 2000 | 2250 | 2500 | 2750 | 3000 | 3250 | 3500 | 3750 | 4000 | 4250 | 4500 | 4750 | 5000 | 5250 | 5500 | 5750 | 6000 | 6250 | 6500 | 6750 | 7000 | 7250 | 7500 | 7750 | 8000 | 8250 | 8500 | 8750 | 9000 | 9250 | 9500 | 9750 | 10000 | 10250 | 10500
Chart: Vickers Hardness [HV]
W
Mo
Ta
4 mm of
gradient
thickness

## Slide 21: Conclusion
WAAM is able to manufacture solid large-scale structures in refractory metals by fusion;
WAAM is able to create functionally graded structure (FGS) is a controlled way;
WAAM is able to control the evolution of the microstructure by monitoring the thermal cycles during deposition;
WAAM is able to improve and manipulate the mechanical properties using in-situ cold work;
WAAM is able to obtain a potential massive cost saving.
Future work:
Tungsten thermo-mechanical tests;
Tungsten residual stresses measurements;
Production of large parte in tantalum;
Fine tuning of the gradient of the FGS;
High-resolution DIC tensile test for the FGS.

## Slide 22
Visit our web page: waammat.com
Gianrocco Marinelli
g.marinelli@cranfield.ac.uk
Thank you for the attention